Fragments of

THE RECORD OF HISTORY AND CULTURE RESTORATION MONUMENT (MOVABLE)

Icon “Assumption of the Blessed Virgin Mary”

National Academy of Fine Arts and Architecture

Institution where the conservation treatment was performed

Department of Techniques and Restoration of Art Works

department

1. Typological affiliation of the monument

| Type of monument | monuments of Fine Art | monuments of Decorative Art | archaeological monuments | paper monuments | Other monuments of history and culture |
| --- | --- | --- | --- | --- | --- |
| Icon Definition, nature of the monument | 1 | 2 | 3 | 4 | 5 |

| 2. Place of permanent storage, owner of the monument | Private collection, Kyiv, Ukraine |
| --- | --- |

| 3. Data about the monument |  |  |  | notes, clarifications |
| --- | --- | --- | --- | --- |
| artist |  | Unknown |  |  |
| name | Assumption of the Blessed Virgin Mary |  |  |  |
| Date of creation | 19 century |  |  |  |
| Base, materials | Canvas, oil |  |  |  |
| techniques | oil painting |  |  |  |
| size | 70 х 61cm |  |  |  |

| 4. The reason for conservation |  | Unsatisfactory condition, deformation of the base due to lack of frame and improper storage, severe cracking and breakthrough. Loss of paint layer together with the gesso. |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  | Reasons and aims for conservation-restoration treatment |  |  |  |
| Letter-statement of the owner and the decision of the restoration council. Bringing to an expositional look. |  |  |  |  |  |
| Name of the document, date, number |  |  |  |  |  |
| Monument was given for treatment 26.01.2018 |  |  |  |  | Restorer-conservator Antonina Mykolaichuk |
| Date of the conservation treatment completion 25.06.2018 |  |  | 4th year student conservator-restorer Conservator’s category |  |  |

5. Basic data on the history of the monument, historical information, information on storage conditions, preliminary restorations and research, the source of this information.

The owner did not provide any information about the origin of the icon.

6. The state of the monument at the time of receipt for restoration

a) by visual observation:

Frame:

The frame is missing. The presence of holes from the nails suggests that the canvas was attached to the frame.

Base:

The icon is painted on canvas. The size of the icon is 60.4 x 70.5 cm. The canvas is linen, thin, fine-grained, and manufactured. Linen weaving, density: 14x14 threads in 1 cm2. Probably the canvas was larger, because the edges are cut in some places. The condition of the canvas is unsatisfactory.

Defects:

The canvas is dilapidated. There is a breakthrough in the upper right corner of the canvas (2.9 x 1.3 cm). We observe warping of a canvas on perimeter, folds from external edge of a stretcher, and also an accurate cut from the left side of a canvas. There are 15 holes from nails around the perimeter. The base is tightly covered with dust on both sides.

Gesso :

Gesso was applied by hand, medium thickness, in light ochre. On visual inspection, probably it is chalk glue. The structure is fine-grained. The texture is smooth. The connection with the base is unsatisfactory. Gesso loss is approximately 8%. The main losses of gesso along the perimeter of the icon occurred due to improper storage of the canvas without a frame.

Craquelures:

Present on the entire surface of the canvas with the base. In shape it is  with raised edges - roof-like. It is Strongly expressed. Craquelures of gesso origin, which arose as a result of subsidence of the canvas which is in its turn the result of improper storage conditions.

Paint layer:

Paint layer is oil, multilayer, medium-textured with some thickenings in light areas of painting. The technique of multi-layered painting is used: light brown underpainting, more textured basic color painting layer and final glazing. On the halo of the Mother of God we observe leaf gilding, probably laid on oil varnish.

Preservation is unsatisfactory, there are minorscratches and scuffs in the areas of thinned color painting layer. The connection of the paint layer with the gesso is satisfactory, losses in places of mechanical damage; the area of ​​losses of the paint layer corresponds to the area of ​​gesso losses ≈ 8%. Craquelure is medium reticulate with raised edges of gesso origin.

Covering layer:

Thin, yellowish, uneven, probably resinous.

Surface contamination:

Surface contamination: On the front side, a significant amount of dust contamination. There is a slight degree of diffusion into the layers below. There are numerous fly feces.

On the reverse side: Significant thickness of continuous dense dust and mud contaminants over the entire area of the canvas. There are numerous fly feces.

b) According to laboratory tests:

| # | Purpose and type of research | Description and results of the study | and date of conclusion Storage location | Performer: position, surname, initials, signature |
| --- | --- | --- | --- | --- |
| 1 | Optical and physical research | Under the microscope ochre red underpainting is observed in places of abrasion, destruction and yellowing of the varnish. It is multilayer painting | 05.06.18 | 4th year student Antonina Mykolaichuk |
| 2 | Research in UV rays using a fluorescent lamp Ultralight system "T8 18w / BLB" to detect traces of previous restoration interventions | UV luminescence revealed a blue glow of the varnish over the entire surface of the icon. We can observe dark spots (fading luminescence) in places of recordings with bronze paint: halos, candle flames, on the clothes of Archangel Michael, chaotic spots on the perimeter from the painting of the frame | 06.06.18 | 4th year student Antonina Mykolaichuk |

c) General conclusion about the condition of the monument:

The icon arrived in unsatisfactory condition. The canvas is carelessly cut from the frame; there is a breakthrough, loss of gesso together with the paint layer, a strong medium mesh craquelure, yellowing of the varnish layer. There is dense dust contamination on both sides of the canvas and late records with bronze paint. The monument needs a set of urgent conservation and restoration treatment measures.

7. Conservation Treatment Plan.

The program is based on the task for restoration, adopted by the Restoration Council

Departments of Technology and Restoration of Art Works Minutes #11 dated 26.02. 2018

Restoration Council Secretary Natalia Moskalenko Head of the Department M.F.Tytov

а) Conservation Treatment Plan and the sequence of conservation-restoration measures

1. Adding base loss using “butt” (edge-to-edge) technique  with polyvinyl butyral (PVB).

2. Stretch the painting on the working frame.

3. Restore the connection between the base, gesso and paint layer, using the method of applying reinforcing tape, ironing craquelure.

4. Remove dirt from the reverse side of the canvas.

5. Glue the reverse side of the canvas for duplication.

6. Prepare a duplicating canvas on the working frame.

7. Duplicate the canvas on a new base.

8. Remove the reinforcing tape.

9. Stretch the painting on the museum frame.

10. Apply the restoration gesso in places of loss of painting.

11. Clear the paint layer from surface contamination (remove spot contamination, traces of fly feces).

12. Remove late records of bronze pigment paint.

13. Thin the yellowed varnish layer.

14. Apply a layer of isolating varnish.

15. Tinting (toning) places of loss of painting.

16. Apply a protective layer of varnish.

9. Records of the conservation-restoration plan fullayerent

| # | Description of treatment, indicating the method, technology of materials and tools, and accompanying illustrative materials | Chemicals/materials/ tools | Dates | Who performed |
| --- | --- | --- | --- | --- |
| 1 | 2 | 3 | 4 | 5 |
| 1 | The breakthrough was treated by the method of "butt" (edge-to-edge), using 10% solution of polyvinyl butyral (PVB) in ethyl alcohol, hemp fiber and pre-glued canvas. Flax fiber, saturated with PVB (10%), was smoothed with a fluoroplastic spatula, and then with a warm iron. The loss of the canvas was restored by inserting a pre-glued (2 gelatin sizing with honey 1: 1) linen cloth, graininess and texture similar to the artist's, by the method of "butt" using PVB and fluoroplastic spatula. | PVB 10% solution in ethyl alcohol, hemp fiber, canvas | 23.02.18 | Supervisor: Lush V.V. Scientific consultant: Iryna Somyk-Ponomarenko Conservator-restorer: Antonina Mykolaichuk |
| 2 | Stretched the canvas on the working frame, using strips of сraft paper. The edges of the canvas were pre-ironed, warm gelatin glue was applied and glued cigarette paper was applied to them. After drying the edges, сraft paper was glued on them, then moistened and stretched on the working frame. | Gelatin solution 5% Craft paper | 26.02.18 |  |
| 3 | A reinforcing layer was applied to a 6% solution of gelatin and honey (1: 1), with an antiseptic - zinc acetate Zn (O2CCH3)2 (2% of the dry weight of the adhesive). The solution was applied with a brush on sigarrete paper and painting, then the glued tissue paper was heated with an infrared lamp, after which the craquelure was inserted with a fluoroplastic spatula and an iron, the final stage was ironing the glued painting with an iron through a fluoroplastic layer to evaporate the excess condensate. | 6% solution of gelatin + honey (1: 1) with antiseptic zinc acetate Zn (O2CCH3)2 2% (by dry weight of glue), distilled water | 09.03.18 |  |
| 4 | Removal of dense surface contaminants on the reverse side was performed using a solution of flour paste 10% with antiseptic Zn (O2CCH3)2 (2% of dry weight) mechanically, using a scalpel. The flour paste solution was applied with a brush onto the canvas, after which the dirt was removed with a scalpel. After the paste cleaning was done, the rest dirt and dust was removed with a damp cloth and a scalpel. | solution of flour paste 10% with antiseptic Zn (O2CCH3)2, scalpel, distilled water | 12.03.18 – 26.03.18 |  |
| 5 | Preparation of the reverse side for duplication was performed with a solution of animal glue 8% with honey (1: 1). Using a brush, the glue was applied over the entire surface of the canvas and dried with an iron through a fluoroplastic film until completely dry. | 8% solution of animal glue with honey and antiseptic Zn (O2CCH3)2 | 04.04.18 |  |
| 6 | Preparation of a duplicating canvas for duplication. The canvas was stretched on the working frame and glued three times with a solution of animal glue 8% and honey (1: 1). (The first applying of glue was performed without adding honey). | 8% solution of animal glue with honey (1: 1) and antiseptic Zn (O2CCH3)2 | 06.04.18- 10.04.18 |  |
| 7 | Duplication of the canvas was performed using a solution of animal glue 10% with honey (1: 1) and antiseptic (zinc acetate). The glue solution was applied with a brush on the entire surface of the reverse side of the artist's canvas and duplicating canvas. After the glue became sticky, the canvases were put on each other. With the help of a roller, air was squeezed out through the filter paper and the canvases were rolled with a roller to each other. Then the duplicated canvases were ironed through the filter paper until no condensation. Duplication was completed by ironing through the fluoroplastic film on the side of the paint layer. | 10% solution of animal glue with honey and distilled water with antiseptic | 12.04.18 |  |
| 8 | Removal of reinforcing tape. Cigarette paper was steamed with a sponge and hot distilled water. Excess glue was removed with wet swabs, excess moisture was removed. | Hot distilled water, sponge, cotton swabs | 18.04.18 |  |
| 9 | The canvases were stretched on the museum frame with the help of vices and nails. |  | 20.04.18 |  |
| 10 | Applying of restoration gesso in places of losses. Gesso composition: warm 5% gelatin glue with honey (1: 1) and antiseptic and chalk. The gesso was applied in 2-3 steps with a spatula and a scalpel to the areas of loss. Excess gesso was removed with a scalpel, wet cotton swabs and a cotton cloth. Cork was also used to level the restoration gesso. | 5% gelatin glue with honey (1: 1) and antiseptic Zn(O2CCH3)2, dispersion chalk distilled water | 23.04.18 – 11.05.18 |  |
| 11 | Cleaning the paint layer from surface contaminants was performed with cotton swabs, soap lather (soap that does not contain alkalis) and distilled water. Traces of fly feces were dissolved with a solution of dimethylacetamide with turpentine (1: 1) and removed mechanically with a medical eye scalpel. | baby soap, distilled water, cotton wool, solution of dimethylacetamide and turpentine (1: 1) | 11.05.18-14.05.18 |  |
| 12 | Areas of the late records by bronze paint and random layers around the perimeter of the canvas were dissolved with a solution of dimethylacetamide with turpentine (1: 1) and removed mechanically with a medical eye scalpel. | solution of dimethylacetamide with turpentine (1: 1) | 15.05.18 – 25.05.18 |  |
| 13 | Thinning of the yellowed varnish layer was performed by using a solution of dimethyl sulfoxide with turpentine (1: 1) and cotton swabs. | solution of dimethylacetamide and turpentine (1: 1) | 04.06.18 – 05.06.18 |  |
| 14 | The surface of the painting was covered with an insulating layer of varnish with a cotton swab and a solution of damar varnish + turpentine (1: 1) | damar varnish + turpentine (1: 1) | 05.06.18 |  |
| 15 | Tinting (toning) in places of loss of the artist's painting was performed with low-fat oil paints and restoration paints, with the reconstruction of lost fragments of images. | oil paints and restoration paints | 07.06.18 - 25.06.18 |  |
| 16 | The surface of the painting was covered with a protective layer of varnish with the help of a cotton swab and a solution of damar varnish + turpentine (1: 1) | damar varnish + turpentine (1: 1) | 26.06.18 |  |

10. Illustrative material (photos, cartograms, diagrams, etc.)

Before restoration:

- General view of the icon in direct light, front side;

- Fragment of an icon in direct light 1;

- Fragments of the icon in direct light2;

- Fragments of the icon in direct light 3;

- General view of the icon in side lighting, front side;

- Fragments of the icon in side lighting 1;

- Fragment of an icon in side lighting 2;

- Fragment of an icon in side lighting 3;

- General view of the icon on the reverse side in direct light;

- General view of the icon on the reverse side in side lighting.

In the process of restoration:

- General view of the icon on the reverse side during the clearing process;

- General view of the icon in direct light, after applying the restoration gesso, in the process of removing thick contaminants;

- Fragments of the icon in direct light, after applying the restoration gesso, in the process of removing thick contaminants 1;

- A fragment of the icon in direct light, after applying the restoration gesso, in the process of removing thick contaminants 2;

- A fragment of the icon in direct light, after applying the restoration gesso, in the process of removing thick contaminants 3;

- Photofixation of the front side of the work in UV rays.

- Fragments of the icon in UV rays 1;

- Fragment of the icon in UV rays 2;

- Fragment of the icon in UV rays 3;

- General view of the icon in the process of removing late records with bronze paint.

- Fragments of the icon in the process of removing late records with bronze paint 1;

- Fragment of the icon in the process of removing late records with bronze paint 2;

- Fragment of the icon in the process of removing late records with bronze paint 3;

- General view of the icon after regeneration of the varnish layer;

- Fragments of the icon after regeneration of the varnish layer 1;

- Fragment of the icon after regeneration of the varnish layer 2;

- Fragment of the icon after regeneration of the varnish layer 3;

- General view of the icon after thinning of the varnish layer and covering the icon with an insulating layer of varnish (before tinting).

- Fragments of the icon after thinning of the varnish layer and covering the icon with an insulating layer of varnish (before toning) 1;

- Fragment of the icon after thinning of the varnish layer and covering of the icon with an insulating layer of varnish (before toning) 2;

- Fragment of the icon after thinning of the varnish layer and covering the icon with an insulating layer of varnish (before toning) 3;

After conservation and restoration:

- General view of the icon in direct light;

- Fragment of the icon 1

- Fragments of the icon 2

- Fragments of the icon 3

- General view of the icon on the reverse side in direct light;

11. Results of the conservation-restoration treatment (the description of changes of a technical condition and external changes of a monument after restoration, specification of attributions, etc.)

As a result, in the process of conservation and restoration, the integrity of the base was restored: the loss of the canvas was supplemented; the connection between the base, the gesso and the paint layer was restored. The dirt and dust was removed as well as the 20th century oil-based bronze pigment repainting. Craquelure was flattened, the process of duplication was carried out on a new base and the canvas was stretched on a museum frame. Restoration gesso has been brought to the places of painting losses with subsequent toning, surface contamination and painting with bronze paint were removed, and yellowish varnish layer was thinned. As a result of conservation and restoration measures, the monument was given an expositional look.

12. Recommendations for storage conditions of the monument

1. Maintain the level of relative humidity of 50-55% in the storage at a temperature of + 17to19 ° C;

2. Daily fluctuations in relative humidity should not exceed 5%;

3. Prevent direct sunlight on the artwork;

4. Maintain cleanliness in storage;

5. Avoid drafts.